# IR camera and pyrometer used for woodworking control

by M.Kastek, H.Madura, H.Polakowski and W.Sokołowski2

Military University of Technology, 2 S. Kaliski St. 01-489 Warsaw, Poland

2 Warsaw Agricultural University, Wood Technology Faculty 26/30 Rakowiecka Str., 02-528 Warsaw, Poland

Abstract

## Similarly as metal cutting machines, wood cutting machines can be also equipped with automatic devices for determination of tools conditions. The paper presents one of the methods used for determination of limits of woodworking parameters or admissible wear of blades of cutting tools. The paper includes the results of measurements of woodworking process and other wood materials by means of continuo measurement of a surface temperature by means of IR camera and pyrometer.

1. Introduction

Similarly as metal cutting machines, wood cutting machines can be also equipped with automatic devices for determination of tools conditions. The paper presents one of the methods used for determination of limits of woodworking parameters or admissible wear of blades of cutting tools.

Determination of tool blade wear during a cutting process is extremely difficult. As we know there is a close relation between of cutting process temperature and degree of blade’s wear. Temperature measurement of tool blade used for woodworking is an appropriate factor of the process control.

During machine cutting the balance between temperature of tool blade and temperature on the surface of the worked material is observed. A temperature measurement of the worked material enables determination temperature and technical conditions (degree of wear) of a cutting tool [1].

The paper includes the results of measurements of woodworking process and other wood materials by means of continuo measurement of a surface temperature by means of IR camera and pyrometer.

2. Measurements of temperature changes by means of IR camera

Figure1 presents the control stand. The camera is situated next to milling machine and its optical axis covers with a working plane of a cutting tool. The worked elements were moved by means of a cylindrical, universal feed mechanism along a guide which was made for the experiment. In the guide a rectangular hole was drilled for observation of the treated surface just behind a milling cutter.

IR Inframetrics 760 camera was used for the measurements. The chosen images of temperature area (for temperature range from 17,9( C to 29,3( C with accuracy (0.2( C) were registered on a videotape and in a computer memory.

In the analysis of termovision images the temperatures distribution was registered a line parallel to feed direction, in the working plane of the cutting toll (i.e., half-way thickness of the worked element).

Figure 2 presents temperatures distribution on the worked wooden board with the use of a sharp and blunt blade. The measurements were carried out for the same type of wood and at the same cutting velocity and rate of travel of the worked board. The results of experiment showed a considerable temperatures difference of the worked surface with the use of a sharp or blunt blade. Thus measurement of temperatures distribution can be applied for determination of technical condition of a tool while woodworking or other wooden materials treatment [2].

For temperature determination in diagnosis IR pyrometer can be used. Such pyrometer is cheaper than IR camera. Pyrometer parameters must be adequate for travel rate of the worked material and small measurement area should be only near a cutting tool. Due to high degree of dust the pyrometer should be protected from it by applying additional supply ventilation for pyrometer lens.

Furthermore, the pyrometer should be fixed in another arrangement than woodworking machine one so that it should not undergo machine vibrations. Picture 1 presents the pyrometer constructed for woodworking process control.

3. Temperature measurement by means of pyrometer

For experiments a pyrometer constructed on the basis of smart measuring head and software of the RAYTEK was used. This device allows for remote temperature measurement with accuracy 1% and resolution of 0.1( C. Diameter of measuring area is 6,4 mm (for the distance of 200 mm). Spectral range of the device is within 8-14 (m, what significantly eliminates the influence of external disturbances on the accuracy of measurement. Additionally, the pyrometer was equipped with laser diodes (670 nm) indicating precisely the place of measuring area and autonomous air ventilation on optical elements allows for proper work of the device dustiness. Picture 2 shows the pyrometer on the measuring position.

Temperature measurements were carried out while milling fibreboard of medium density (MDF). The large width (thickness) of shavings causes disturbances of a cutting process because of additional material squashing by the shavings. As a result of material squashing and at the same increase in power of a friction force additional heat is produced. The aim of experiments was to determine the influence of the shavings width on temperature of the worked surface.

Figure 3 present heating of worked surface as cutting distance increases while milling MDF with the use of tools with the same blades of various values of shavings width. Figure 4 presents the change of medium temperature depending on the shavings width [1].

Temperature measurements of the worked surface obtained by the use of pyrometer indicate that it is possible to determine the degree of tool’s wear as well as to establish permissible values of cutting process. Temperature value of the worked surface can be the basic signal for automatic control system of woodworking and at the same allows for wood working control.

4. Conclusions

The experiments have shown usefulness of IR pyrometer for continuos temperature measurements of the worked surface while milling wood and wooden materials. Additionally it was concluded that while diagnosis of wood and wooden materials treatment that temperature measurement of the worked surface only is not sufficient one. For example in experiments of shavings width influence of tool with the same blades on the temperature of the worked surface determination of adequate shavings width for proper cutting process be confirmed by experiment results of cutting forces distribution. Only then it is possible to provide exact data for practical application tools with the same blades application.

The experiments have also shown that as tools wear increases a temperature of the worked surface increases as well. It is obvious, and carpenters commonly know this phenomenon. Work with blunt tool causes burns and even carbonisation of the worked elements. The application of IR pyrometers for determination of limits of cutting tools wear allows for automation of this process. Temperature of the worked surface and values of cutting forces are optimum input signals for smart systems of woodworking monitoring and in particular for determination of limits of a blades wear of cutting tool.

Further experiments are planned purpose of which is determination of influence of blades wear degree on temperature of the worked surface. The developed infrared pyrometer will be used to determine temperature value.

REFRENCES

[1] Madura H, Polakowski H, Kastek M. 1996. Diagnostyka procesu obróbki drewna metodami radiometrycznego pomiaru temperatury. Pomiary Automatyka Kontrola.

[2]  Sokołowski W. 1995a. Zastosowanie kamery termowizyjnej w badaniach procesu obróbki drewna i tworzyw drzewnych. V Konferencja Naukowo - Techniczna. Obróbka Matriałów Niemetalowych NM ’95. Rzeszów, październik 1995.

Fig .1 Control stand: 1-milling machine, 2-feed mechanism, 3-worked element, 4-guide, 5-slot for observation of the treated surface, 6-IR camera.

Fig.2 Temperature of the surface of worked wood measured close the cutting tool: 1-blunt tool 2-sharp tool.

Fig.1. IR pyrometer constructed for woodworking process control

Fig.2. IR pyrometer on the measuring position

Fig.3. Relation between the value of shaving width and the temperature of worked surface

Fig.4. Relation between the value of shaving width and the medium temperature of worked surface