# Non-destructive evaluation and thermal diffusivity estimation with averaged infrared thermography measurements: application to stratified systems

by E. Poncet1, D. Béreiziat 1, G. Grangeot 1 and J.-C. Batsale 2

1U.F.C. - I.G.E., Parc Technologique - 2, Av. Jean Moulin, 90000 Belfort, France ;

2L.E.P.T.- E.N.S.A.M. (U.R.A. C.N.R.S. 873), Esplanade des Arts et Métiers, 33405 Talence Cedex, France

Abstract:

## Estimation methods are proposed for thermal characterization of stratified systems by means of quantitative infrared measurements. Two thermal configurations are studied with an averaging point of view for a stratified system composed of two layers. The principle of the estimation method is based on the use of Taylor developments of the non-linear analytical transform solutions to apply linear estimators and fit spectral distributions or time evolutions of experimental macroscopic temperature data. The straight potential industrial and laboratory applications are respectively non-destructive thermal evaluation of delaminations in composite laminate and thermophysical characterization, i.e., diffusivity identification.

1. Introduction

Unlike to contact sensor systems, infrared temperature measurements can provide a lot of data useful for accurate quantitative characterization of plane systems [1, 2], if the measurement noise of the IRT camera is strongly reduced. Averaging processes allow such a noise reduction when averaged temperature fields are computed from infrared temperature fields.

In this paper, two methods are proposed for thermal characterization of stratified systems from averaged temperature data. The configurations of the thermal problems, i.e., steady or transient heat conduction with uniform heat losses, are described by analytical solutions obtained with integral transform methods in the Fourier or Laplace spectral domains. These solutions are linearized on the basis of a Taylor expansion to provide approximate models well suited to methods of linear parameter estimation. The so-obtained analytical identification function involves the thermal properties of both phases and a possibly thermal contact resistance, which are directly linked to the averaged temperatures of the phases. Therefore averaged temperature data are exploitable to compute the estimation of these parameters. Averaging processes of temperature fields measured with an infrared camera are appropriate to these averaging descriptions of the heat transfer. The aim of these new techniques is to propose analytical and direct methods for stratified systems characterization at room temperature. The main advantage of such methods is to process a great number of data in order to reduce the effect of the measurement noise on the estimation result. Application fields of the non-destructive thermal evaluation of delaminations in composite laminate and thermophysical characterization are concerned by these methods. Indeed, thermal properties of homogeneous media or thermal contact resistance in stratified composites can be determined with a simple experimental fitted sample, since neither the knowledge of the heat flux excitation, nor a sophisticated insulating apparatus is required.

2. Thermal problem

We treat the heat diffusion problem for a stratified medium with the geometrical features represented in Fig. 1. We consider two stagnant phases adjacent with a perfect conducting contact or a uniform thermal contact resistance Rc. The parallelepiped system is submitted to a continuous or transient local heat source Q1 on the 1-phase and to uniform heat losses (xy-planes) characterized by a convective heat coefficient hc, so that the fin hypothesis is verified. We solve the steady and transient three-dimensional analytical problems and develop the corresponding analytical transformed solutions. We consider both layers made of homogeneous, isotropic solids with temperature-independent properties. The above thermal problem yields to the following differential equation system:

(1)-(2)

where , the temperature increase above the initial temperature for the i-layer, is a function of the three space variables (x, y, z) and time variable t.

The initial temperature field is spatially uniform and the x and y-ends boundary conditions are lateral adiabatic walls,

, ,  and 	   (3)

xy-planes uniform heat losses are characterized by a single convective heat coefficient hc on the upper (z= e) and lower (z = 0) faces and the fin hypothesis along z-direction is assumed:

and 	(4)

At the interface A12 (y = e1) of the phases, the perfect (Rc = 0) or resistive contact leads to:

and

at A12 	(5)

This equation system is solved by suitable integral transform methods for the steady or the transient heat diffusion processes to define a common analytical relationship between averaged temperatures of both phases and the macroscopic thermal impedance Z:

with 	(6)

where (2 is the generalized frequency of the 2-phase given by:

- for the steady state case:

(7)

with (j  the discrete Fourier frequency.

- for the transient case:

(8)

with p  the Laplace variable.

We introduce the first order term of the Taylor expansion of the impedance Z for both frequencies (1 and (2 small and we obtain an analytical relationship between the temperature transform ratio, (1, (2 and Rc:

(9)

with R the intrinsic macroscopic resistance of the bimodal system.

Therefore, experimental determination of the global resistance (R + Rc) is feasible, provided that experimental temperature data are exploitable with the suited identification method in the frequency space. However, more terms in the Taylor expansion have to be considered for reliable estimations of the parameters [2] because of the reduced validity frequency range of the equation (9). In the next sections, we present the experimental validations of two methods for both transient or steady heat conduction processes on samples without thermal interfacial resistance (Rc = 0).

3. Experimental setup

Steady heat transfer measurements are performed on a stainless steel sample (3 mm thick, 42 mm wide, 655 mm long) and transient ones on steel (1 mm thick, 58 mm wide, 1000 mm long). Each sample is heated on its half width, so that it stands for the two phases. The black painted front face of the slab is scanned with a 4 up to 25 frames per second rate by an infrared camera (Avio 2002 ST). The infrared radiometer is fitted with an array of ten Stirling cycle cooled Indium Antimonide sensors. The (256(100) temperature values of each frame are stored in a real-time memory, so that 512 frames of the steady or transient temperature field can be successively recorded.

It’s assumed that emissivity of the black coated surface is uniform to avoid systematic measurement errors. The heat source is a flat electric heating element dissipating several Watts and glued on the rear face of the 1-phase. Experiments are made at constant room temperature but room temperature varies from one experiment to another. Physical locations of the sample are established through visualization of low emissivity markers on the recorded frames. Both temporal and spatial averaging treatments of the thermal field are performed by the use of the computing environment Matlab [3].

A statistical noise characterization is carried out for a large number of experimental temperature measurements. Errors on measured temperatures by infrared thermography are well known to be characterized by a zero mean and a constant standard deviation. However, statistical independence property assumption must be verified. Several experimental determinations of the covariance matrix of the averaged temperature error vector are performed for a set of N (= 512) recorded infrared frames in the uniform temperature field case. 				Calculations of the covariance matrix confirm the independence characteristic of the errors. Indeed, covariance values are negligible compared to variance ones.

4. Steady state inverse problem

The approximate transform solution is obtained in the Fourier frequency space and the following identification function is deduced:

(10)

where (m are the identifiable parameters of the linear model (N( = 10) and (, ) are the intrinsic integral cross-sectional (over y variable) averaged temperatures.

Therefore, estimation of R may be processed in the Fourier space for a given number of discrete (j values with infrared temperature fields. These experimental noisy data are characterized by additive independent errors with a quantifiable diagonal covariance matrix (see previous section). Thus, we use the maximum likelihood estimator [4] with minimal variance to identify the parameters (m.

In Figs. 2-3, an experimental temperature field and its associated macroscopic temperature distributions have been obtained with 512 infrared frames averaged over time to reduce the temperature noise. In the Fig. 4, a good agreement between experimental results of R estimations (versus (j) and simulated ones shows that the method is appropriate to thermal resistance evaluation with infrared measurements for the low frequency range since the signal over noise ratio tends towards unity for higher frequencies.

5. Transient inverse problem

The identification function is defined in versus the Laplace variable (N( = 6):

(11)

In the case of transient heat conduction, (, ) are the intrinsic integral temperatures averaged over y and x space variables so that experimental transient macroscopic temperature evolutions can be obtained from transient infrared temperature fields.

The classical least squares method is used to compute the first approximate set of estimated parameters in the Laplace domain with the thermal diffusivity:

(12)

An iterative procedure (Simplex algorithm [4]) allows determining precisely the thermal diffusivity of the sample. The so-obtained macroscopic temperature evolutions (see Fig. 5) are fitted in the time domain with the theoretical ones  which are obtained by the convolution product between the experimental evolution and the inverse Laplace transform of the theoretical function .

The estimated diffusivity values of the steel sample are in good agreement with the flash method measurements (a = 1.8 10 –5 m/s2 with a relative standard deviation lower than 10 %).

REFERENCES

[1] L. Ramond, J.C. Batsale, C. Gobbé and M. Quintard, Measurement of a thermal exchange coefficient in porous media by infrared thermography- Two-temperature model application, Inter. Heat  Transfer Conf. 11, 1998, Kyongju, Korea.

[2] E. Poncet, D. Béreiziat, P. Fallot, G. Grangeot and J.C. Batsale, Two-medium treatment of heat transfer in stratified media: experimental estimation of the heat exchange coefficient by infrared thermography measurement, submitted to Inter. J. Heat and Mass Transfer.

[3] Matlab Reference Guide, The MathsWorks, Inc., 24 Prime Park Way, Natick, Mass. 01760.

[4] W.H. Press, B.P. Flannery, S.A. Teukolsky and W.T. Vetterling. Numerical recipes, 1989, Cambridge University Press, London.

FIGURES

Fig. 2. Steady state thermal experiment : Infrared temperature frame after time averaging process (stainless steel sample).

| Fig. 3 Steady state thermal experiment : spatial distributions of the cross sectional averaged temperatures (stainless steel sample) | Fig. 4 Steady state experiments : experimental and simulated estimations (stainless steel sample) |
| --- | --- |
| Fig. 5 Transient thermal experiment : evolutions of the surface averaged temperatures (steel sample) |  |

# Text boxes

# Free convection

heat losses (hc)

# Free convection

heat losses (hc)

e1

n12

next

# 2-phase

# 1-phase

L

e1 + e2

e

z

y

x

Fig. 1 . Geometry and boundary conditions of the system.

Adiabatic walls

Local heated zone